# X-GRASS LAWN / RYE

# Technical Data

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Fiber Type |  |  | 100% Thiolon Polyethylene Mono |
| Fiber Mass | 7500 monofilament | 8300 d tex monofilament | 6 ply |
| Pile Height * | 2.0 in | 50.8 mm |  |
| Color (s) |  |  | Evergreen |
| Tufting Gauge ** | 3/8 |  |  |
| Stitch Rate ** | 11.5 / 3 in. | 1.51 / cm |  |
| Primary Backing | 6.5 oz/yd² | 220 g/m² | Stabilized dual layered woven polypropylene |
| Secondary Backing | 8.5 oz/yd² | 288 g/m² | DuraFlo |
| Non Woven Scrim | 2.5 oz/yd² | 85 g/m² |  |
| Optional Secondary Min. footage required | 20.0 oz/yd² | 678 g/m² | Urethane- Scrapecoat with perforations |

| Property | Imperial Unit | Metric Unit | Test Method |
| --- | --- | --- | --- |
| Face Weight | 45.0 oz/yd² | 1526 g/m² | ASTM D418 |
| Total Weight, Dura Flo | 62.5 oz/yd² | 2119 g/m² | ASTM D418 |
| Total Weight, Urethane | 71.5 oz/yd² | 2424 g/m² | ASTM D418 |
| Permeability |  |  | DIN 18-035, part 6 |
| Tuft Bind | 9 lb – f | 40 n | ASTM D1335 |
| Grab Tear MD | 200 lb | 91 kg | ASTM D5034 |
| Grab Tear CMD | 200 lb | 91 kg | ASTM D5034 |
| Infill Amount, recommend | ¾ of Pile Height |  |  |

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Item Number, Dura Flo |  |  | EL45 |
| Item Number, Urethane |  |  | XT45 optional |
| Roll Width | 15 ft. | 4.57 m |  |
| Roll Length *** | 100 ft. | 30.5 m |  |
| Area per Roll *** | 1500 ft.² | 139.4 m² |  |
| Total Roll Weight, Dura Flow | 651 lbs. | 295 kg |  |
| Total Roll Weight, Urethane | 745 lbs. | 338 kg |  |

# Text boxes

Product Properties

Performance Properties

Packaging

X-Grass® Worldwide

Synthetic Turf Solutions

P. O. Box 579

Rocky Face, GA 30740

Ph: 877-881-8477