# ST70 / X-GRASS TOUR FRINGE 70

# Technical Data

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Fiber Type |  |  | 100% Thiolon Polyethylene Mono / KDK |
| Fiber Mass | 7500 den monofilament 4000 den KDK Root Zone | 8300 d tex monofilament 4800 d tex KDK Root Zone | 6 ply mono slit film KDK per needle |
| Pile Height * | 1 9/16 in | 39.6 mm |  |
| Color (s) |  |  | Evergreen |
| Tufting Gauge ** | ½ |  |  |
| Stitch Rate ** | 15.5 / 3 in. | 2.03 / cm |  |
| Primary Backing | 6.5 oz/yd² | 220 g/m² | Stabilized dual layered woven polypropylene |
| Secondary Backing | 20.0 oz/yd² | 678 g/m² | Urethane-Scrapecoat with perforations |
| Optional Secondary Min. footage required | 8.5 oz/yd² | 288 g/m² | Dura Flo |
| Non Woven Scrim | 2.5 oz/yd² | 85 g/m² |  |

| Property | Imperial Unit | Metric Unit | Test Method |
| --- | --- | --- | --- |
| Face Weight | 70.5 oz/yd² | 2390 g/m² | ASTM D418 |
| Total Weight, Urethane | 97.0 oz/yd² | 3289 g/m² | ASTM D418 |
| Total Weight, Dura Flo | 88.0 oz/yd² | 2984 g/m² | ASTM D418 |
| Permeability |  |  | DIN 18-035, part 6 |
| Tuft Bind | 9 lb – f | 40 n | ASTM D1335 |
| Grab Tear MD | 200 lb | 91 kg | ASTM D5034 |
| Grab Tear CMD | 200 lb | 91 kg | ASTM D5034 |
| Infill Amount, recommend | ¾ of Pile Height |  |  |

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Item Number, Urethane |  |  | ST70 |
| Item Number, Dura Flo |  |  | EL70 optional |
| Roll Width | 15 ft. | 4.57 m |  |
| Roll Length *** | 100 ft. | 30.5 m |  |
| Area per Roll *** | 1500 ft.² | 139.4 m² |  |
| Total Roll Weight, Urethane | 1010 lbs. | 458 kg |  |
| Total Roll Weight, Dura Flo | 916 lbs. | 415 kg |  |

# Text boxes

Product Properties

Performance Properties

Packaging