# XTRB / Rye Blend

# Technical Data

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Fiber Type |  |  | 100% Polyethylene |
| Fiber Mass | 10800 den | 11400 dtex | Monofilament Blend |
| Pile Height * | 2.0 in | 50.8 mm |  |
| Color (s) |  |  | TWEED |
| Tufting Gauge ** | 3/8 |  |  |
| Stitch Rate ** | 8.5 / 3 in | 1.12 / cm |  |
| Primary Backing | 7.0 oz/yd² | 237 g/m² | Stabilized dual layered woven polypropylene |
| Secondary Backing | 8.5 oz/yd² | 288 g/m² | Dura Flo |
| Non Woven Scrim | 2.5 oz/yd² | 84.8 g/m² |  |

| Property | Imperial Unit | Metric Unit | Test Method |
| --- | --- | --- | --- |
| Face Weight | 42.0 oz/yd² | 1424 g/m² | ASTM D418 |
| Total Weight | 60.0 oz/yd² | 2034 g/m² | ASTM D418 |
| Permeability | TBD | TBD | DIN 18-035, part 6 |
| Tuft Bind | 6 lb - f | 27 n | ASTM D1335 |
| Grab Tear MD | N/A |  | ASTM D5034 |
| Grab Tear CMD | N/A |  | ASTM D5034 |
| Infill Amount, recommend | ¾ of Pile Height |  |  |

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Item Number |  |  | XTRB |
| Roll Width | 15 ft. | 4.57 m |  |
| Roll Length *** | 100 ft. | 30.5 m |  |
| Area per Roll *** | 1500 ft.² | 139.1 m² |  |
| Total Roll Weight | 625 lbs. | 284 kg |  |

# Text boxes

Product Properties

Performance Properties

Packaging